|  |  |  |
| --- | --- | --- |
| C:\Users\hp-pro\Downloads\tompon_jmes1.jpg | **J. Mater. Environ. Sci., 2021, Volume 12, Issue xx, Page xxxx-xxxx**  <http://www.jmaterenvironsci.com> | **Journal of Materials and**  **Environmental Science**  **ISSN : 2028-2508**  **CODEN : JMESCN**  **Copyright © 2021,**  **University of Mohammed Premier**  **Oujda Morocco** |

# Production of Hybrid Biochar by Retort-Heating of Elephant Grass for Waste Management and Product Development

**A. G. Author1\*, J. O. Author 1,2\*\*, D. V. Author1, A. O. Author 1**

*1Department of Chemical Engineering, Faculty of Engineering and Technology, University of xxxx, Bity, P.M.B.1515, Country*

*2Department of Chemical Engineering, Jilali University, P. M. B. 5025, New Caty, Country*

*\*Corresponding author, Email address:*

*\*\*Corresponding author, Email address:*

**Abstract**

In a bid to achieve energy and environmental sustainability research efforts are now being channeled to product development from waste materials especially in developing countries. The aim of this study was to convert.

Received xx Aug 2021, Revised xx xxx 2021, Accepted xx xxx 2021

*Keywords*

* *Biomaterial*
* Fuel,
* Lipide,
* Energy,
* Waste.

*abcdefg.arb@newfric.edu Phone: +7;*

# 1. Introduction

Solid waste management a major challenge of the 21st century due to increasing population, urbanisation and lifestyle changes due to technological development [[1](#_ENREF_1)]. This problem is even more pronounced in developing countries such as Nigeria where solid waste management is a major concern [[2](#_ENREF_2),3]. With increasing global change pressures coupled with existing un-sustainability factors, cities in developing countries are most likely to experience difficulties in efficiently managing municipal solid wastes. Municipal solid waste management constitutes one of the most crucial health and environmental problem facing African cities [[4](#_ENREF_4)]. Most cities spend 20-50% of their annual budget on solid waste management [[5](#_ENREF_5)] and only 20-80% of the waste is collected [[6](#_ENREF_6)]. The waste density ranged from 280 to 370 kg/m3 and the waste generation rates ranged from 0.44 to 0.66 kg/capita/day [[7](#_ENREF_7)]. Pyrolysis is a way to utilise the carbon in plants before it can become a meal for eaters and return it to the soil as pure carbon biochar [[8](#_ENREF_8)]. Pyrolysis mimics the natural process that turned ancient plants into coal: When biomass is heated up with no oxygen supply it melts into carbon, syngas and bio-oil [[9](#_ENREF_9)]. Almost the same solutions are proffered to management of LDPE which include biodegradation in a solid waste medium [[10](#_ENREF_10)], pyrolysis, gasification and carbonisation.

In this study, elephant grass (*Pennisetum Purpureum*) was co-carbonised with low density polyethylene (LDPE) to produce hybrid biochar in a top-lit updraft biomass conversion reactor using the method described by ... In the method, an updraft gasifier with retort heating was used. The goal of the process is two-pronged. Firstly, the management of plastic wastes. Secondly is the energy conservation from the plastic and the readily available biomass to produce valuable products.

# 2. Methodology

## 2.1 Sourcing and preparation of

Dried sample of … These were also locally sourced.

## 2.2 Experiments

Details of experiments are exactly as those described in previous reports [[17](#_ENREF_17), [18](#_ENREF_18)]. The biomass conversion was conducted in the 48.5 cm high reactor with full dimensions and schematics provided elsewhere [[17](#_ENREF_17)]. The hybrid co-conversion of biomass and plastic was conducted in the 53 cm high reactor with full dimensions and schematics provided elsewhere [[18](#_ENREF_18)].

The reactors consist of a centrally oriented conversion chamber within its’ set-up and possessing several small air holes at the base. The chamber houses the feed to be converted while the combustion fuel for heat generation occupies the ‘heating gap’ between the chamber and the reactor itself.

## 2.3 Product characterisation

The products (biomass biochar and hybrid biochar) recovered from the process were characterised to ascertain some of their properties using Scanning Electron Microscope with energy Dispersive X-ray Spectroscopy (SEM-EDS), Fourier Transform Infra-Red Spectroscopy (FTIR) and Brunauer-Emmet-Teller (BET) analysis. Scanning Electron Microscopy (SEM, Phenom proX, Phenom-World BV, Netherlands) was used to study the surface morphology of the particles of the biochar. A double adhesive was placed on a sample stub. The sample was sprinkled on the sample stub and subsequently taken to a sputter coater (quorum-Q150R Plus E) and coated with 5 nm of gold. The sample was placed on a charge reduction sample holder and introduced into the column of the SEM machine. It was firstly viewed with a NavCam before being sent to SEM mode. The acceleration voltage of the microscope was set to 15 kV and magnification at 1000 – 1500×. FTIR (Shimadzu, FTIR-8400S, Japan) was used to determine the functional groups and complexes present in both biochar samples. The surface area, pore volume and size of the chars were measured. The surface properties of the char samples were studied using a Multipoint BET surface area and the DR (Dubinin–Radushkevic) method for the pore volume and width (diameter). The chars were characterized by N2 adsorption test at 77 K. 100 ml/min of dry nitrogen was introduced into the sample tube to prevent contamination of the clean surface, then the sample tube was removed and the sample weighed. The sample tube was fixed to the volumetric apparatus, and then the sample was evacuated to 2 Pa pressure. Adsorbate was introduced to give the lowest desired relative pressure, and then the volume adsorbed was measured.

# 3. Results and Discussion

## 3.1 Temperature profile

Temperature readings were taken at the various points Tb, Tm, Tt, and Ti for each of the reactor at a time interval of 10 minutes to generate a temperature profile along the time of carbonisation. Tb, Tm, Tt, and Ti represents temperatures at the bottom (side), middle (side), top (side) and within the reactors respectively. The initial set of temperature measurements was done before ignition and the final set was done when the system had come into equilibrium with atmospheric conditions.

**Figure 1a.** Temperature profile for biomass conversion

**Figure 1b.** Temperature profile for hybrid co-conversion

## 3.2 Product yield

The bio-char yield for both processes was computed using the system of equations in **Eqn. 3** [[18](#_ENREF_18)].

**Eqn. 1**

**Eqn. 3**

Where M1 = mass of conversion chamber + Feed (in grams), M2 = mass of conversion chamber (in grams), M3 = ….summarised in **Table 1**.

**Table 1.** Summary of reactor performance

|  |  |  |
| --- | --- | --- |
| **Index** | **Biomass conversion** | **Hybrid co-conversion** |
|  |  |  |

The biomass biochar yield of 13.8 wt% (at 371oC peak temperature) in this study is similar to the 14.29 wt% (at 300oC peak temperature) obtained for the same feedstock in a previous investigation [[17](#_ENREF_17)].. This was confirmed by the EDS results.

## 3.3 Product composition

The composition of the products was determined using Energy Dispersive X-ray spectroscopy (EDS). The spectrums are shown in **Figures 2a-b** and the results summarised in **Table 2**. The only major component missing is Hydrogen. From the results in **Table 2**, it can be observed that the hybrid

**Table 2.** Major elemental composition of the biomass and hybrid biochar

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **S/N** | **Element** | **Biomass Biochar** | | **Hybrid Biochar** | |
| **Atomic Conc.** | **Weight Conc.** | **Atomic Conc.** | **Weight Conc.** |
| 1 | Carbon | 74.13 | 57.79 | 86.89 | 75.46 |
| 2 | Silicon | 9.63 | 17.55 | 1.95 | 3.95 |
| 3 | Potassium | 4.17 | 10.57 | 3.46 | 9.79 |
| 4 | Oxygen | 9.57 | 9.94 | 4.59 | 5.31 |
| 5 | Nitrogen | 0.85 | 0.78 | 1.26 | 1.27 |
| 6 | Chlorine | 0.38 | 0.89 | 0.50 | 1.29 |
| 7 | Calcium | 0.26 | 0.67 | 0.25 | 0.72 |
| 8 | Aluminum | 0.33 | 0.57 | 0.26 | 0.50 |
| 9 | Phosphorus | 0.26 | 0.52 | 0.26 | 0.58 |
| 10 | Magnesium | 0.26 | 0.40 | 0.28 | 0.50 |
| 11 | Sulfur | 0.12 | 0.24 | 0.19 | 0.44 |
| 12 | Sodium | 0.06 | 0.08 | 0.11 | 0.18 |

**Figure 2a.** EDS spectrum for biomass biochar

**Figure 2b.** EDS spectrum for hybrid biochar

## 3.4 Biochar surface morphology

The surface morphology of the products was determined using SEM. **Figures 3a-b** and **4a-b** shows the SEM micrographs of the (see **Table 2**).

**Figure 3.** SEM micrograph of biochar, at (a) 1000× and (c) 1500×

**Figure 4.** SEM micrograph of hybrid biochar, at (a) 1000× and (c) 1500×

## 3.5 Biochar functional groups

**Table 3** shows the functional groups of raw ….correspond to the alkoxyl (C-OH) group [[25](#_ENREF_25)].

**Table 3.** Summary of observed peaks and assignments

|  |  |  |  |  |
| --- | --- | --- | --- | --- |
|  |  | | | **References** |
|  |  |  |
|  |  |  |  | [[17](#_ENREF_17)] |
|  |  |  |  | [[23](#_ENREF_23), [25](#_ENREF_25)] |
|  |  |  |  | [[22](#_ENREF_22)] |
|  |  |  |  | [[22](#_ENREF_22), [23](#_ENREF_23)] |
|  |  |  | [[26](#_ENREF_26)] |
|  |  |  |  | [[27](#_ENREF_27)] |
|  |  |  |  | [[28](#_ENREF_28)] |
|  |  |  |  | [[17](#_ENREF_17)] |

**Figure 5.** FTIR spectrum of raw biomass

The peak 1635 cm-1 observed in the biomass spectra which shifted to 1620 cm-1 and 1573 cm-1 in biomass. Retort heating also underlines the usability of the process even in remote locations or in on-site applications [[37](#_ENREF_37)].

# Conclusion

The co-conversion cost, high biochar yield and no electrical power requirement. The study has been able to successfully achieve the co-conversion of biomass and plastics (as typologies of MSW major components valuable products with a twin goal of waste management and product development.

# Acknowledgement

# The technical inputs of Mr xxxx of Mechanical Engineering Department are acknowledged.

# Disclosure statement: *Conflict of Interest:* The authors declare that there are no conflicts of interest.

*Compliance with Ethical Standards:* This article does not contain any studies involving human or animal subjects.

# References

[1] D. Hoornweg and P. Bhada-Tata, *What a waste: a global review of solid waste management* vol. 15: World Bank, Washington, DC, 2012. http://hdl.handle.net/10986/17388

[2] E. Amasuomo, and S. A. Hasnain, "Analysis of public participation in sustainable waste management " *Environmental Management and Sustainable Development,* 4 (2015)180.

[3] O. Amuda, S. Adebisi, and A. Alade, "Challenges and possible panacea to the solid wastes management" *Journal of Sustainable Development Studies,* 6 (2014) 64-70.

[4] B. Abila and J. Kantola, "Municipal solid waste management problems solution," in *Proceedings of World Academy of Science, Engineering and Technology*, (2013) 292.

[5] A. A. Adelodun, and L. T. Arowoyele, "Thermochemical conversion of oil palm Fiber-LDPE hybrid waste" *Biofuels, Bioproducts and Biorefining,* https://doi.org/10.1002/bbb.2130

[6] K. A. Ayuba, A. H. Sabrina, and S. W. N. Azmin, "Current status of municipal solid waste management practise," *Research Journal of Environmental & Earth Sciences,*  5 (2013) 295-304.

[7] T. Ogwueleka, "Municipal solid waste characteristics and management in Nigeria," *Journal of Environmental Health Science & Engineering,* 61 (2009) 73-180.

[8] J. O. Ighalo and A. G. Adeniyi, "An In Silico Temperature Sensitivity Study of the Pyrolysis of Beech," *European Journal of Sustainable Development Research,* 4 (2020) 1-7.

[9] T. R. Blakeslee, "Biochar: The Key to Carbon-Negative Biofuels," *Renewable Energy World,* 4 (2009) 2009.

[10] S. Zahra, S. S. Abbas, M.-T. Mahsa, and N. Mohsen, "Biodegradation of low-density polyethylene (LDPE) by isolated fungi in solid waste medium," *Waste management,* 30 (2010) 396-401.

[11] O. J. Ajala, J. O. Ighalo, A. G. Adeniyi, S. Ogunniyi, and C. A. Adeyanju, "Contamination issues in sachet and bottled water in Nigeria: a mini-review," *Sustainable Water Resources Management,* 6 (2020) 112.

[12] J. O. Ighalo and A. G. Adeniyi, "A Comprehensive Review of Water Quality Monitoring and Assessment in Nigeria," *Chemosphere,* 260 (2020) 127569.

[14] J. O. Ighalo, A. G. Adeniyi, J. A. Adeniran, and S. Ogunniyi, "A systematic literature analysis of the nature and regional distribution of water pollution sources in Nigeria," *Journal of Cleaner Production,* 2020. https://doi.org/10.1016/j.jclepro.2020.124566

[15] E. Quartey, H. Tosefa, K. Danquah, and I. Obrsalova, "Theoretical framework for plastic waste " *International journal of environmental research and public health,* 12 (2015) 9907-9919.

[16] K. Kato, S. Nomura, and H. Uematsu, "Development of waste plastics recycling process using coke ovens," *ISIJ international,* 42 (2002) S10-S13.

[17] A. G. Adeniyi, J. O. Ighalo, and D. V. Onifade, "Production of biochar from elephant grass (Pernisetum purpureum) using an updraft biomass gasifier with retort heating," *Biofuels,* 2019. https://doi.org/10.1080/17597269.2019.1613751

[18] A. G. Adeniyi, J. O. Ighalo, and D. V. Onifade, "Production of Bio-char from Plantain (Musa paradisiaca) fibers using an Updraft Biomass Gasifier with Retort Heating," *Combustion science and technology,* 2019. https://doi.org/10.1080/00102202.2019.1650269

[19] S. A. Abdulkareem, J. O. Ighalo, D. V. Onifade, and S. K. Sanusi, "Thermochemical Co-conversion of Sugarcane Bagasse-LDPE Hybrid Waste into Biochar," *Arabian Journal for Science and Engineering,* 2020. https://doi.org/10.1007/s13369-020-05119-9

[20] T. E. Odetoye, J. Titiloye, and J. O. Ighalo, "A Thermodynamic Study Of Rice Husk (Oryza Sativa) Pyrolysis," *European Journal of Sustainable Development Research,* 3 (2019) 1-10.

(2021) ; <http://www.jmaterenvironsci.com>